## Slide 1: Modeling and Simulation of Magnetic Transmission Lines
Muhammad Shamaas
2018-MS-EE-4
Supervisor: Dr. Muhammad Asghar Saqib

## Slide 2: Research Objectives
Model dispersive, inhomogeneous, gyromagnetic and lossy Magnetic materials.
Study equivalent magnetic circuits for ferromagnetic transmission lines using
  DC Magnetic Reluctance Model for a cumulatively compounded 1800 rpm, 40V low voltage, low power DC generator.
  Low frequency (150 kHz) Permeance-Capacitance Model for a small length (0.1 m i.e. about at 150 kHz) pulse transformer used in a 160 / 5 V, 100 A, low voltage, low power, isolated, full bridge buck converter.
  High frequency (1 MHz – 1 GHz) Magnetic Transmission Line model for a small length (30 cm i.e. 1λ at 1 GHz), dispersive, gyromagnetic, Ferromagnetic core used in a low voltage, low power pulse transformer simulated using Finite Difference Time Domain (FDTD) Simulator MEEP.

## Slide 3: 1. Introduction to Magnetic Transmission

## Slide 4: 1. Introduction to Magnetic Transmission Lines
Magnetic Transmission Lines transmit information through Magnetic Flux which acts as the effective Magnetic charge. Time varying magnetic flux results in a Magnetic Displacement Current inside the Transmission Line.
The operation of a Magnetic Transmission Line does not involve flow of magnetic or electric charges. They are very poor electrical conductors. However, changing Magnetic Fields produce Electric Fields which is stored in the dielectric medium.
Together, the Electric and Magnetic Fields transmit Energy along the direction of propagation.

## Slide 5: 1. Applications of Magnetic Transmission Lines
Inductors and Magnetic Amplifiers.
Filters and Pulse Transformers.
Alternating Current and Direct Current Machines.
Magnetic Memory, Spintronic and Nanomagnetic Logic Devices
Directional Couplers and Magnetometers.
Induction Heaters and Magneto-resistive Sensors.
Gyromagnetic Devices, Microwave generators and Magnetic Resonance Imaging.

## Slide 6: 1. Applications of Magnetic Transmission Lines

## Slide 7: 1.1. Introduction to Solid State Magnetism

## Slide 8: 1.1. Magnetization and Permeability
Magnetic Fields originate from movement of bound charges (orbital electrons, electron spin and nuclear spin). This movement results in a bound current.
An electron in an atomic orbital possesses a Magnetic Moment due to its rotation in a loop (orbital moment) and spin around an axis (spin moment).
  where I is the bound current, A is the loop area, is the gyromagnetic ratio and L is the angular momentum of the electron.
3. Magnetization M is the total magnetic dipole moment per unit volume.
=

## Slide 9: 1.1. Properties of Magnetic Materials
 | Magnetic Moments | Susceptibility
Diamagnetism | no magnetic moment | Small & negative, - to -
Paramagnetism | randomly oriented | Small & positive, to
Antiferromagnetism | antiparallel aligned | Small & positive, to
Ferrimagnetism | mixed parallel and antiparallel aligned | large (below ), to
Ferromagnetism | parallel aligned | large (below ), to
 | Magnetic Moments | 
Diamagnetism |  | 
Paramagnetism |  | 
Antiferromagnetism |  | 
Ferrimagnetism |  | 
Ferromagnetism |  | 

## Slide 10: 1.1. Sample Materials for Manufacturing Magnetic Transmission Lines
The following materials can be used for manufacturing Magnetic Transmission Lines.
Ferromagnetic materials: Iron, Nickel, Cobalt, Manganese alloys e.g. NiFe, , MnSb, MnAs, MnZn, CuAl.
Ferrimagnetic materials: Iron, Nickel, Cobalt, Zinc, Manganese, Aluminium alloys e.g. , Pb, B, NiO, ,.
They have a permeability that can be very high at dc, but decreases quickly with increasing frequency according to Snoek’s law. These materials are electric insulators or semiconductors.
Source: https://www.researchgate.net/publication/321357089_Magnetic_material_selection_for_EMI_filters/figures?lo=1

## Slide 11: 1.1. Magnetic Susceptibility
When a ferromagnetic material is magnetized, the susceptibility follows the a non-linear curve.
When the material is saturated, the magnetic susceptibility becomes zero.
Besides Magnetic Field Intensity, permeability is strongly dependent on chemical composition, crystal structure, stress, temperature and time after magnetization

## Slide 12: 1.1. Magnetic Hysteresis
Ferromagnetic materials are non-linear as their permeability varies with the strength of applied field intensity.
The flux in a ferromagnetic material depends on the instantaneous Magnetomotive force and its history.
At high magnetic field intensity, the material saturates, limiting further increase of Magnetic Flux.

## Slide 13: 1.1. Dielectric and Diamagnetic Losses
During Lorentz resonance, lattice vibrations or electronic resonance, the harmonic oscillations become extreme. The in-phase flux cancels the anti-phase flux so the observed permittivity and permeability drops.

## Slide 14: 1.1. Other Losses in Magnetic Cores
Non-linear, Frequency dependent energy loss effects in magnetic materials:
Core Residual Loss
Core Eddy Current Loss
Conductance Loss
Skin Effect Loss
Proximity Effect Loss
Self Capacitance Dielectric Loss
Self Capacitance Circulating Currents Loss

## Slide 15: 2. Magnetic Circuit Modeling

## Slide 16: 2. Three Magnetic Circuit Models
This chapter discusses three magnetic circuit models for Ferromagnetic Transmission Lines:
DC Non-linear Reluctance Model
Low Frequency Permeance-Capacitance Model
High Frequency Magnetic Transmission Line Model

## Slide 17: 2.1. Magnetic Reluctance Model

## Slide 18: 2.1. Complex Magnetic Reluctance Model for Magnetic Circuits

## Slide 19: 2.1. Complex Magnetic Reluctance Model for Magnetic Circuits
H. A. Rowland’s Law (1873) is the counterpart of G. Ohm’s Law (1827) for Magnetic circuits. Complex Reluctance Model defines Magnetic reluctance as the ratio of sinusoidal Magnetomotive Force and sinusoidal Magnetic Flux.
Lossy Complex Magnetic Reluctance is non-linear and varies with the magnetic field. It resists Magnetic flux.

## Slide 20: 2.1. Inconsistency in Complex Magnetic Reluctance Model
In 1969, R. W. Buntenbach proved that the model is not power invariant. Reluctance Power Loss cannot be calculated using Joule Heating Law (1842) Analogy due to dimensional inconsistency:
Hence this is not an accurate model for Power and Energy Flow.

## Slide 21: 2.1. Reluctance model for a Compounded DC Generator
1. Electric System
2. Magnetic System
3. Relation between Electric and Magnetic System

## Slide 22: 2.1. Simulation of Reluctance model for a Compounded DC Generator
Parameters:
RA=0.19 Ω
RS=0.02 Ω
RF=20-50Ω
NF=1000 turns
NS=2000 turns
Rated speed=1800 rpm.
Rated Voltage=40 V.

## Slide 23: 2.1. Simulation of Non-Linear Reluctance
Reluctance is a function of Magnetic Voltage.
Magnetic Flux is given by

## Slide 24: 2.1. Simulation of Non-Linear Reluctance

## Slide 25: 2.1. Simulation of Reluctance model for a Compounded DC Generator
The rotor mechanical speed was increased from 1000 to 2500 rpm in steps of 250rpm.
Reluctance model is only suitable for steady state simulations of machines if the reluctance profile of the magnetic core and the voltage/ flux relation is known.

## Slide 26: 2.2. Permeance-Capacitance Model

## Slide 27: 2.2. Tellegen’s Gyrator theory (1948)
B. Tellegen’s Gyrator theory (1948) can describe power invariant transformation of magnetic and electric quantities. The dual effort and flow quantities are related by the gyration constant N.

## Slide 28: 2.2. Tellegen’s Gyrator (1948)
The gyrator transforms magnetic displacement current (rate of change of magnetic flux) into induced electric voltage.
The gyrator transforms electric conduction current into generated Magnetomotive force.

## Slide 29: 2.2. Validation of Gyrator Theory (1948)
M. Faraday’s Law (1831): The rate of change of magnetic flux penetrating a closed loop is responsible for the induced electromotive force in the loop.
A. Ampere’s Law (1861): The Electric conduction current flowing through a closed loop is responsible for generating Magnetomotive force in the loop.

## Slide 30: 2.2. Power Invariant Permeance-Capacitance Model (1969)
R. W. Buntenbach proposed Power Invariant Permeance-Capacitance Model (1969) to replace Reluctance Model.
Magnetic Displacement Current is the rate of change of Magnetic Flux which results from the polarization of Magnetic Dipoles.

## Slide 31: 2.2. Magnetic Permeance
Magnetic Permeance is defined as the inverse of the Magnetic reluctance.
It represents an equivalent magnetic capacitor which stores magnetic flux (measured in Volt.seconds).
The Permeance Magnetic displacement current (measured in Volts) is proportional to the Permeance and the rate of change of Permeance Magnetic voltage (measured in Amperes).

## Slide 32: 2.2. Permeance-Capacitance Model for a full bridge Isolated Buck Converter

## Slide 33: 2.2. The switching table for the switches and diodes
 | Transistors |  |  |  | Diodes | 
Time Interval | T1 | T2 | T3 | T4 | D1 | D2
 | ON | OFF | OFF | ON | ON | OFF
 | OFF | ON | OFF | ON | ON | ON
 | OFF | ON | ON | OFF | OFF | ON
 | ON | OFF | ON | OFF | ON | ON
 | Transistors |  |  |  | Diodes | 
Time Interval | T1 | T2 | T3 | T4 | D1 | D2
 | ON | OFF | OFF | ON | ON | OFF
 | OFF | ON | OFF | ON | ON | ON
 | OFF | ON | ON | OFF | OFF | ON
 | ON | OFF | ON | OFF | ON | ON

## Slide 34: 2.2. The design parameters
Parameter | Symbol | Value
Source Voltage |  | 160 V
Load 1 Voltage |  | 5 V 5%
Load 1 Current |  | 100 A 5%
Core cross-sectional area |  | 2.26cm2
Core Magnetic Path Length |  | 9.58 cm
Peak Flux Density |  | 0.08 T
Core relative Permeability |  | 3500
Core Resistivity |  | 0.02 Ωm
Switching Frequency |  | 150 kHz
Duty Cycle | D | 0.75
Parameter | Symbol | Value
Source Voltage |  | 160 V
Load 1 Voltage |  | 
Load 1 Current |  | 
Core cross-sectional area |  | 2.26cm2
Core Magnetic Path Length |  | 9.58 cm
Peak Flux Density |  | 0.08 T
Core relative Permeability |  | 3500
Core Resistivity |  | 0.02 Ωm
Switching Frequency |  | 150 kHz
Duty Cycle | D | 0.75

## Slide 35: 2.2. The Design Procedure
1. Applied Primary winding flux
2. Turns of Primary winding
3. Turns of Secondary windings
4. Core Permeance
5.Core Resistance
6. Load Filter Design
,

## Slide 36: 2.2. Permeance-Capacitance Model for a full bridge Isolated Buck Converter

## Slide 37: 2.2. Model for Primary winding gyrator

## Slide 38: 2.2. Model for Secondary winding gyrators

## Slide 39: 2.2. Model for non-linear Permeance

## Slide 40: 2.2. Sample Response of non-linear Permeance

## Slide 41: 2.2. Simulation Model of full bridge Isolated Buck Converter

## Slide 42: 2.2. Source and Load waveforms

## Slide 43: 2.2. Permeance Magnetic Voltage and Magnetic Displacement Current
The Permeance-Capacitance model uses a non-linear Permeance to model nonlinearity and hysteresis losses of magnetic materials.
It is valuable for simulating transient behavior of Ferromagnetic elements like RF inductors, transformers and filters.

## Slide 44: 2.3.Magnetic Transmission Line Model

## Slide 45: 2.3. Magnetic Transmission Line Model (2012)
J. A. B. Faria and M.P. Pires presented Magnetic Transmission Line Model (2012) based on Electric Transmission Line Model in terms of per unit length Transverse Impedance and per unit length Longitudinal Admittance.

## Slide 46: 2.3. Distributed Parameters in Magnetic Transmission Line Model (2012)
Per unit length Magnetic Conductance, Magnetic Inductance and Magnetic Capacitance are defined as:

## Slide 47: 2.3. Energy Loss and Energy Storage in Magnetic Transmission Line Model (2012)
1. Energy is dissipated in Magnetic Conductance due to skin effect.
2. Electrical Energy is stored in Magnetic Capacitance; and Magnetic Energy is stored in Magnetic Inductance.
3.The Magnetic Transmission Line Equations can be solved just like Electric Transmission Line Equations.

## Slide 48: 2.3. Lossy Transmission Lines
Electric Transmission Line | Magnetic Transmission Line
Electric Transmission Line | Magnetic Transmission Line

## Slide 49: 3. Electromagnetic Simulations and MEEP Simulator

## Slide 50: 3.1. Finite Difference Time Domain Method

## Slide 51: 3.1. Finite Difference Time Domain Method (1966)
K. S. Yee’s Method (1966) or Finite Difference Time Domain Method is a differential numerical modeling technique for computational electrodynamics.
J. C. Maxwell’s Equations (1861) are discretized using central difference approximations to the space and time partial derivatives. For example,
where n represents the discrete time step.

## Slide 52: 3.1. Yee Lattice (1966)
Finite Difference Time Domain Method discretizes space into a grid of small elements called Yee Lattice (1966). The different field components at a grid location are stored in the edges and faces of a cubic element. They are evolved in discrete time steps.

## Slide 53: 3.2. Introduction to MEEP Simulator

## Slide 54: 3.2. Introduction to MEEP Simulator
MEEP (2006) is a script based Simulator for modeling the time domain and frequency domain behavior of a variety of arbitrary materials including anisotropic, dispersive, non-linear and gyrotropic media.
C++ interface: Features variable resolution and normalized units.
Material Library: Sample data for several materials is provided in libraries for building accurate test structures.
Current Sources: A wide variety of electric or magnetic current sources can be simulated.
Derived components: Electric/ Magnetic/ Thermal Energy Density, Poynting Flux etc. can be evaluated.
Mathematical operations: Averaging, symmetry and integration are allowed in cylindrical and rectangular coordinates.
Data Visualization: The fields can be printed as image or video files.

## Slide 55: 3.2. MEEP: Boundary Conditions
The finite region of space must always be terminated with some boundary conditions. Three types of terminations are supported:
Bloch-periodic Boundaries: These are used for simulation of periodic structures . Periodic Bloch Boundaries copy the field component at one cell’s edge and reinject them at a neighboring cell’s edge.
Metallic Walls: All fields are forced to be zero at the boundaries (perfect reflector has zero absorption and zero skin depth).
Perfectly Matched Layers: All the fields pass through the open boundary with no reflection. These absorbing boundary layers (ABC) absorb all incident fields.

## Slide 56: 3.2. MEEP: Material Inhomogeneity
and can vary with position inside a material. They can be declared at each individual point in space using a function.
1-D, 2-D and 3-D simulation is possible. Hence every space vector can have up to three spatial coordinates.
The simulation can be carried out in rectangular or cylindrical coordinates. Hence different homogeneous/inhomogeneous structures can be built inside the space.
Symmetry can be used to create complex geometries as well.

## Slide 57: 3.2. MEEP: Material Nonlinearity
The Pockels and Kerr Non-linearity model (1875) explains how can change as a function of the field intensity.
sum is the Pockels effect constant; whereas sum is the Kerr effect constant.
Ferromagnetic materials are non-linear as their permeability varies with the strength of applied field intensity. At high magnetic field intensity, the material saturates, limiting further increase of Magnetic Flux. Hence, the susceptibility decreases rapidly.

## Slide 58: 3.2. MEEP: Dispersion of Permeability
Drude-Lorentzian Model (1900) for frequency dependent permittivity and permeability. Flux Densities contain terms for infinite frequency response and frequency dependent Polarization vector.
is represented as a sum of a resonance term and a term for frequency independent permeability.
couples the polarization to the driving field, is the angular resonance frequency,is the damping factor.

## Slide 59: 3.2. MEEP: Gyromagnetism
Gyrotropic Drude-Lorentz model describes the precessional motion of magnetic dipoles in a static magnetic field.
describes the linear deviation of magnetization from its static equilibrium value. Precession occurs around the bias vector.couples the polarization to the driving field, is the angular resonance frequency,is the damping factor.
For ferromagnetic media biased in the z-direction b=b , a non-diagonal susceptibility tensor is used to relate Magnetization and Field intensity.
, = , = , =

## Slide 60: 3.2. MEEP: Gyromagnetism
The Larmor Precession Frequency for some magnetic materials placed in a static magnetic field.
Material | Larmor Frequency at
Manganese – 53 | 10.94 MHz
Iron – 57 | 1.38 MHz
Cobalt – 59 | 10.07 MHz
Nickel – 61 | 3.81 MHz
Zinc – 67 | 2.66 MHz
Material | 
 | 10.94 MHz
 | 1.38 MHz
 | 10.07 MHz
 | 3.81 MHz
 | 2.66 MHz
Source: http://kodu.ut.ee/~laurit/AK2/NMR_tables_Bruker2012.pdf

## Slide 61: 3.2. MEEP: Transmittance Spectra
Broadband response: The 3 Dimensional Discrete Fourier transform (1822) of the response to a short impulse can give useful information about the transmitted power and losses.
The Transmitted Power can be computed using the integral of Poynting Vector (1884); over a surface on the far end of the transmission line.
Transmitted power and incident power can be used to find power losses in transmission line.

## Slide 62: 3.3. MEEP Simulation of Dispersive, Gyromagnetic Ferromagnetic Transmission Line

## Slide 63: 3.3. MEEP Simulation for Magnetic Transmission Line
The Magnetic Transmission Line consisted of a Gyromagnetic, dispersive ferromagnetic core used in a microwave frequency pulse transformer.
The Transmission Line was excited using a small Gaussian soft electric current source.
Temporal and Spatial resolution
The multi-dimensional discrete Fourier transform (1822) was used to determine the Broadband Response and transmission line parameters.

## Slide 64: 3.3. Introduction to Pulse Transformer
A pulse transformer passes a frequency band and is designed to handle complex waveforms like rectangular pulses.
It is used for impedance matching, voltage/ current transformation, DC isolation, mixing, power splitting, coupling and signal inversion.

## Slide 65: 3.3. Pulse Transformer Magnetic Transmission Line Model
The pulse Transformer was made from a ferromagnetic MnZn material hence its behavior was modeled using the Magnetic Transmission Line model.

## Slide 66: 3.3. Pulse Transformer Simulation in MEEP
Build Grid and Geometrical Structures for transformer, windings and boundaries.
Set 𝜀, 𝜇, 𝜎, Material Inhomogeneity, Dispersion and Non-Linearity Model Parameters.
Add volume current sources, set resolution and run Simulation for desired discrete steps.
Apply 3D Discrete Fourier Transform to find transmitted Poynting Flux and Broadband Response.
A pulse transformer was excited by a small Gaussian soft electric current pulse to examine the Frequency Response. The 3 dimensional discrete Fourier Transform was used to determine Broadband Response.

## Slide 67: 3.3. Geometry of Pulse Transformer
A pulse transformer was simulated to study the effects of Magnetic Transmission Lines parameters on its frequency response.
The primary winding was excited by a small Gaussian soft electric current pulse to examine the Frequency Response of electromagnetic power Transmission.
The power received at the secondary side was analyzed by integrating the received Poynting flux.

## Slide 68: 3.3. Material Properties of MnZn Ferrite
Gyrotropic Drude Permeability
Permittivity and Conductivity
Source: http://www.fair-rite.com/76-material-data-sheet/

## Slide 69: 3.3. Susceptibility versus bias
, = , = , =

## Slide 70: 3.3. Soft Electric Gaussian Current Pulse
A Gaussian soft electric current pulse was applied in the primary winding.
The Fourier Transform of the transverse Magnetic Field is shown below for the range of 0 – 1 GHz.

## Slide 71: 3.3. Evolution of Magnetic Voltage and Current

## Slide 72: 3.3. Evolution of Poynting Flux Density

## Slide 73: 3.3. Color map for Longitudinal Fields
 | X ↑ | Y ʘ | Z →
Magnetic Field Intensity H |  |  | 
Magnetic Flux Density B |  |  | 
Electric Field Intensity E |  |  | 
Electric Flux Density D |  |  | 

## Slide 74: 3.3. Color map for Transverse Fields
 | X ↑ | Y → | Z
Magnetic Field Intensity H |  |  | 
Magnetic Flux Density B |  |  | 
Electric Field Intensity E |  |  | 
Electric Flux Density D |  |  | 
 | X ↑ | Y → | 
Magnetic Field Intensity H |  |  | 
Magnetic Flux Density B |  |  | 
Electric Field Intensity E |  |  | 
Electric Flux Density D |  |  | 

## Slide 75: 3.3. Field Map for Magnetic Transmission Line
1. Magnetic Displacement Current
2. External Electric Field
3. External Magnetic Field
4. Propagation Constant
5. Intrinsic wave impedance

## Slide 76: 3.3. Propagation Constant of Magnetic Transmission Line
The propagation constant was calculated by the following relation:

## Slide 77: 3.3. Propagation Constant versus bias
The magnetic bias can be used to modulate the Attenuation Constant and Phase velocity.

## Slide 78: 3.3. Phase Velocity of Magnetic Transmission Line
The phase velocity was calculated by the following relation:

## Slide 79: 3.3. Intrinsic Wave Impedance of Magnetic Transmission Line
The intrinsic wave impedance is given by
𝜂
𝜂
Near 1 GHz, the permeability drops to 1 hence the intrinsic impedance approaches 377 Ohm.

## Slide 80: 3.3. Intrinsic Wave Impedance versus bias
The magnetic bias can be used to modulate the Intrinsic Wave Impedance of the Magnetic Transmission Line.

## Slide 81: 3.3. Longitudinal Admittance of Magnetic Transmission Line
The Longitudinal Admittance was calculated using the following relation:

## Slide 82: 3.3. Longitudinal Admittance versus bias
The magnetic bias can be used to modulate the Longitudinal Admittance. This controls the losses and the bandwidth of the Magnetic Transmission Line

## Slide 83: 3.3. Transverse Impedance of Magnetic Transmission Line
The Transverse Impedance was calculated using the following relation

## Slide 84: 3.3. Transverse Impedance versus bias
The magnetic bias can be used to modulate the Transverse Impedance. This controls the bandwidth of the Magnetic Transmission Line.

## Slide 85: 3.3. Limitations of MEEP simulation
The MEEP simulation was used to study power losses due to conduction of eddy currents, hysteresis loss, core loss and electromagnetic resonance. The results are only valid for small signal analysis of the Gyromagnetic, Dispersive, Ferromagnetic MnZn core.
The MEEP simulator can not be used to model the following magnetic effects:
Magnetostriction effects
Acoustic effects
Quantum Mechanical Effects

## Slide 86: 4. Conclusion

## Slide 87: 4. Comparison of three Models
 | Reluctance Model | Permeance-Capacitance Model | Transmission Line Model
Conserved Quantity | ? | Magnetic Flux [Volt-Second] | Magnetic Flux [Volt-Second]
Flow Variable | Magnetic Flux [Volt-Second] | Rate of change of Magnetic Flux [Volt] | Rate of change of Magnetic Flux [Volt]
Effort Variable | Magnetomotive Force [Ampere] | Magnetomotive Force [Ampere] | Magnetomotive Force [Ampere]
Energy Dissipation Element | Magnetic Reluctance [] | ? | Magnetic Conductance [Ohm]
Electrical Energy Storage Element | ? | ? | Magnetic Capacitance [Farad]
Magnetic Energy Storage Element | ? | Magnetic Permeance [Henry] | Magnetic Inductance [Henry]
 | Reluctance Model | Permeance-Capacitance Model | Transmission Line Model
Conserved Quantity | ? | Magnetic Flux [Volt-Second] | Magnetic Flux [Volt-Second]
Flow Variable | Magnetic Flux [Volt-Second] | Rate of change of Magnetic Flux [Volt] | Rate of change of Magnetic Flux [Volt]
Effort Variable | Magnetomotive Force [Ampere] | Magnetomotive Force [Ampere] | Magnetomotive Force [Ampere]
Energy Dissipation Element |  | ? | Magnetic Conductance [Ohm]
Electrical Energy Storage Element | ? | ? | Magnetic Capacitance [Farad]
Magnetic Energy Storage Element | ? | Magnetic Permeance [Henry] | Magnetic Inductance [Henry]

## Slide 88: 4. Conclusion
The reluctance model is suitable for DC analysis of ferromagnetic materials. A DC Magnetic Reluctance Model for a cumulatively compounded 1800 rpm 40V low voltage/ power DC generator was presented.
The Permeance-Capacitance model is suitable for low frequency analysis of ferromagnetic materials. A Low frequency Permeance-Capacitance Model for 150kHz pulse transformer was used in a 160V to 5 V, 100 A low voltage/ power isolated full bridge buck converter.
The Magnetic Transmission Line Model is suitable for high frequency analysis of ferromagnetic materials. A High frequency low voltage/ power (30 cm i.e. 1λ at 1 GHz) gyromagnetic, dispersive Magnetic Transmission Line was simulated using Finite Difference Time Domain (FDTD) Simulator MEEP to study Frequency Domain Behavior of Magnetic Transmission Line parameters.

## Slide 89: 4. Scope for Further Work
The power invariant Magnetic Transmission Line model can also be used for accurate modeling of
Alternating Current and Direct Current Machines
Nanomagnetic Logic Devices and Magnetic Transistors
Magnetic Memory Devices and Spintronic devices
Circulators, Couplers, Filters, Power Dividers and Waveguides
Gyromagnetic Non-Linear Transmission Line Microwave generators

## Slide 90: References
[1] J. B. Faria, Multimodal propagation in multiconductor transmission lines. J. Electromag. Waves Appl. 2014, p. 1677–1702
[2] J. B. Faria, Formulation of Multiwire Magnetic Transmission-Line Theory, Progress in Electromagnetics Research B, Vol. 49, 2013, p. 177–195.
[3] J. B. Faria, Matrix theory of wave propagation in hybrid electric/magnetic multiwire transmission line systems, Journal of Electromagnetic Waves and Applications, Vol. 29, No. 7, 2015, p. 925–940.
[4] J. B. Faria, A physical model of the ideal transformer based on magnetic transmission line theory, Journal of Electromagnetic Waves and Applications, Vol. 27, No. 3, 2013, p. 365–373.
[5] J. B. Schneider, Understanding the Finite-Difference Time-Domain Method, 2017, p. 33-74.
[6] A. Oskooi, D. Roundy, M. Ibanescu, P. Bermel, J.D. Joannopoulos, and S.G. Johnson, MEEP: A flexible free-software package for electromagnetic simulations by the FDTD method, Computer Physics Communications, Vol. 181, 2010, p. 687-702.
[7] J. B. Faria, Complex reluctance of inhomogeneous Euler-Cauchy tubular ferrites taking into account frequency dependent complex permeability, Progress In Electromagnetics Research M, Vol. 25, 2012, p. 71–85.
[8] C. Paul, K. Whites and S. Nasar, Introduction to electromagnetic fields, 4th ed. Boston: WCB/McGraw-Hill, 1998, p.586-589.
[9] B. Sevcik and L. Brancık, Time-Domain Simulation of Nonuniform Multiconductor Transmission Lines in Matlab, International Journal of Mahematics and Computers in Simulation, Vol.5, No. 2, 2011, p. 1-8.

## Slide 91: References
[10] G. Antonini, A general framework for the analysis of metamaterial transmission lines. Prog. Electromagn. Res. B., 2010, p. 353–373
[11] C. Caloz and T. Itoh, Electromagnetic Metamaterials: Transmission Line Theory and Microwave Applications, Wiley-IEEE Press, 2006, p. 27-58.
[12] IEEE, Standard for Validation of Computational Electromagnetic (CEM) Computer Modeling and Simulation, and Recommended Practice, Part I, IEEE, June 2008.
[13] C. Paul, Introduction to Electromagnetic Compatibility, 2nd ed. Kentucky: John Wiley and Sons, 2006, p. 559-710.
[14] L. Er-Ping, Computational Electromagnetics for Electromagnetic Compatibility/ Signal Integrity Analysis, IEEE EMC DL Talk, University of Missouri, 2008.
[15] T. C. Edwards and M. B. Steer, Foundations for Microstrip Circuit Design, 4th ed. Wiley-IEEE Press, 2016, p. 576-607.
[16] J. Dickens and A. Neuber, Material selection considerations for coaxial, ferrimagnetic-based nonlinear transmission lines, Journal of Applied Physics, 113, 064904, 2013, p. 1-5.
[17] J. Parson, A. Neuber, J. Dickens and J. Mankowski, Investigation of a stripline transmission line structure for gyromagnetic nonlinear transmission line high power microwave sources, Review of Scientific Instruments, 87, 034706, 2016, p. 1-7.
[18] G. Dominguez, Power-Invariant Magnetic System Modeling, PhD Disseration, Texas A&M University, 2011, p. 45-64.